FLAMMABILITY TEST REPORT

JOHN R. COLAO, INC. FAA DER

1299 Wooden Valley Crossroad, Napa Ca. 94558

(707) 425-9666

Job No. 8625		Page 2

Tested By:  John Colao	Test Date:  03/19/10

Customer: Edwards & Associates, Inc. 			Reference:  P.O. # PO105002EA

TEST SPECIMEN:   GPS 695/696 Mount (Air Gizmo)

For Part 27 helicopter

(Test performed: FAR 25.853 12 second Vertical Ignition)

| FAR PART 25 REGULATION SUMMARY |  | TEST REQUIREMENTS - MAXIMUM |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ignition Time - Material Position | Federal Aviation Regulation | Extinguish Time | Burn Length | Drip Extinguish | Burn Rate Average | Flame Penetration | After Glow |
| 60 Second Ignition - Vertical | 25.853 (a)(1)(i) | 15 Sec Avg | 6 In Avg | 3 Sec Avg |  |  |  |
| 12 Second Ignition – Vertical | 25.853 (a)(1)(ii) | 15 Sec Avg | 8 In Avg | 5 Sec Avg |  |  |  |
| 15 Second Ignition – Horizontal | 25.853 (a)(1)(iv) |  |  |  | 2.5 In/Min |  |  |
| 15 Second Ignition – Horizontal | 25.853 (a)(1)(v) |  |  |  | 4.0 In/Min |  |  |
| 30 Second Ignition - 45 Degrees | 25.855 (a)(2)(ii) | 15 Sec Avg |  |  |  | None | 10 Sec |
| 30 Second Ignition - 60 Degrees | 25.869 (a)(4) | 30 Sec Avg | 3 In Avg | 3 Sec Avg |  |  |  |

| TEST RESULTS |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Sample Number | Extinguish Time (Seconds) | Burn Length (Inches) | Drip Extinguish (Seconds) | Grain Direction | Burn Rate (In/Min) | Flame Penetration | After Glow |
| 1 | 10 | 0.75 | ---- | Lay | ---- | ---- | ---- |
| 2 | 7 | 0.75 | ---- | Lay | ---- | ---- | ---- |
| 3 | 4 | 0.75 | ---- | Lay | ---- | ---- | ---- |
| 4 |  |  |  |  |  |  |  |
| 5 |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |
| Average - Lay |  |  |  |  |  |  |  |
| Average - Warp | 7 | 0.75 |  |  |  |  |  |

ITEM PASSED	COMMENTS: